beryllium copper rod

C17200 beryllium copper rod alloy 25 bronze rod bar

The C17200 beryllium copper rod is a type of alloy 25 processing bar. C17200 beryllium copper rod is usually made of c17200 copper and has excellent electrical conductivity, thermal conductivity, corrosion resistance, and processing performance. It is widely used in electronics, electrical engineering, mechanical manufacturing, construction, transportation, aerospace and other fields.

The C17200 beryllium copper rod refer to solid copper rods made through processes such as extrusion, drawing, and rolling. Their cross-sections are mostly circular, but there are also square, hexagonal and other irregular-shaped rods. Beryllium copper rods possess excellent mechanical properties as well as excellent electrical and thermal conductivity, and are important basic materials in modern industry.

Outstanding mechanical properties

High strength: After solution treatment and aging, the tensile strength can reach 1105–1345 MPa, and the yield strength is approximately 1035 MPa. This is much higher than that of ordinary copper alloys, and some of the properties can be comparable to those of special steels.

High hardness: The hardness can reach HRC38–44, with excellent wear resistance, suitable for high-strength and high-friction working conditions.

High elasticity and fatigue resistance: It has excellent elastic limit and fatigue limit, suitable for elastic components that undergo repeated bending and deformation, such as springs, connectors, and micro switches.

C17200 beryllium copper rod （ASTM B196）

C17200/C17300 Common round rod specifications

| D (mm) | L (mm) | T (mm) | w (kg/m) |
| --- | --- | --- | --- |
| 5 | 2000 | +0.10 | 0.167 |
| 6 | 2000 | +0.10 | 0.240 |
| 8 | 2000 | +0.10 | 0.427 |
| 10 | 2000 | +0.10 | 0.668 |
| 12 | 2000 | +0.12 | 0.961 |
| 16 | 2000 | +0.12 | 1.709 |
| 20 | 2000 | +0.15 | 2.670 |
| 25 | 2000 | +0.15 | 4.172 |
| 30 | 2000 | +0.20 | 6.008 |
| 45 | 2000 | +0.25 | 13.528 |
| 50 | 2000 | +0.25 | 16.698 |

Note: ASTM B196 is mainly applicable to beryllium copper alloy rods, for high-precision and high-strength elastic applications. The density is approximately 8.25g/cm³.

Application

Copper bar is widely used in boat building,War industry, Car industry and communication industry where the components need good wear proof and great corrosion resistance.

Beryllium copper plate becu alloy plate blocks

Definition

Beryllium copper plate (also known as beryllium bronze plate or beryllium copper alloy plate) is a copper-based alloy sheet with beryllium (Be) as the main alloying element. The beryllium content is usually between 0.2% and 2.75%. It combines the excellent electrical and thermal conductivity of copper with the high strength, high elasticity, and corrosion resistance of beryllium, making it the "king of elastic non-ferrous metals". It is widely used in high-end industrial fields.

Core feature of Beryllium copper plate

| Feature | Explanation |
| --- | --- |
| High intensity / High hardness | The tensile strength can reach over 1100 MPa, with a hardness of 36 to 44 HRC, comparable to that of special steel. |
| High elasticity | High elastic limit, small elastic lag, outstanding fatigue resistance, suitable for components subjected to repeated forces |
| High conductivity / high thermal conductivity | Conductivity ≥ 18% IACS, thermal conductivity ≥ 105 W/(m·K), excellent heat dissipation and conductivity performance |
| Corrosion-resistant | It is resistant to corrosion in air, fresh water, salt water and sulfuric acid medium. Its lifespan can exceed 40 years in seawater environment. |
| Non-magnetic / No Spark | The impact does not produce sparks and is suitable for explosion-proof safety environments. |
| Good processability | Easy to weld, solder, polish and electroplate, suitable for complex and precise parts |
| Resistant to high and low temperatures | The working temperature range is wide, and it does not become brittle at low temperatures, while maintaining stable performance at high temperatures. |

Common grades and chemical compositions of beryllium copper plates

| grades | chemical compositions（wt%） | others |
| --- | --- | --- |
| C17200 | Be 1.9~2.15, Co 0.35~0.65, Ni 0.20~0.25, Cu remain | High intensity, high conductivity |
| C17300 | Be 1.8~2.0, Co+Ni 0.4~0.6, Pb 0.2~0.6, Cu remain | Easy to machine, high conductivity |
| C17410 | Be 0.4~0.7, Co 2.4~2.7, Ni 0.2~0.3, Cu remain | High thermal conductivity and high strength |

Reference standard：ASTM B196、GB/T 5231、DIN 2.1247 and so on.

Typical performance parameters of beryllium copper plate (taking C17200 as an example)

| Parameters | Numerical value |
| --- | --- |
| Density | 8.25~8.3 g/cm³ |
| Hardness (after aging) | 36~44 HRC |
| Tensile strength | ≥1100 MPa |
| Yield strength | ≥1035 MPa |
| Electrical conductivity | ≥18% IACS |
| Thermal conductivity | ≥105 W/(m·K) |
| Elastic modulus | 128 GPa |
| Melting point | 870~980℃ |

Main applications of beryllium copper plates

Electronics and electrical: High-frequency connectors, contact pads for mobile phone batteries, micro-motor brushes, switches, relays, test probes, etc.

Mold manufacturing: Injection molds, die-casting molds, hot runner nozzles, high-precision inserts, rapid cooling modules.

Aerospace: Engine components, high-temperature bearings, high-strength structural parts.

Marine engineering: Submarine cable repeaters, corrosion-resistant structural parts, deep-sea equipment.

Explosion-proof tools: Spark-free wrenches, hammer heads, etc. safety tools.

Medical devices: Surgical instruments, implants, antibacterial biocompatible components.

The differences between beryllium copper plates and ordinary copper alloys

| Comparison item | Beryllium copper plate | Common brass / copper |
| --- | --- | --- |
| Strength / Hardness | Extremely high, reaching the level of special steel | Lower, much lower than beryllium copper |
| Elasticity/Fatigue Performance | Excellent, does not fail even after repeated deformation | Poor, prone to fatigue |
| Conductive / Thermal Conductive | Good, slightly lower than brass, but much higher than steel | Bronze is the best, followed by brass |
| Corrosion-resistant / Abrasion-resistant | Excellent, suitable for harsh environments | Medium |
| Cost | High | Lower |

Production process and precautions

Main process: Melting → Casting → Hot rolling → Cold rolling → Solution treatment → Aging hardening → Finishing.

Standard

JIS H3250-2006,ASTM B152M,GB/T2040-2008,etc

Size

Thickness:0.1mm~500mm

Width:4mm~2500mm

Length:1m~2m or as required.

Hardness

1/16 hard,1/8 hard,3/8 hard,1/4 hard,1/2hard,full hard,soft,etc

Surface

mill,polished,bright,oiled,hair line,brush,mirror,sand blast,or as required

Package

Standard export package ,or as required.

Application

Used in computer CPU slot,car terminal, cell phone buttons,

electrical connectors and other high-tech electronic field

Characteristics

Excellent cold working performance, high srength and high elasticity, has excellent electroplating,

hot dip andwelding performance, seawater and industrial atmosphere corrosion.

Beryllium copper plate (C17200) standard specifications

| Thickness (mm) | width (mm) | length (mm) | weight (kg/m²) |
| --- | --- | --- | --- |
| 0.5 | ≤300 | ≤1000 | 4.13 |
| 1.0 | ≤300 | ≤1000 | 8.25 |
| 2.0 | ≤300 | ≤1000 | 16.5 |
| 5.0 | ≤300 | ≤1000 | 41.25 |
| 10.0 | ≤300 | ≤1000 | 82.5 |

Description: The density of beryllium copper is approximately 8.25 g/cm³. The thickness is usually between 0.5 and 10 mm, and the width is relatively small, making it suitable for high-precision elastic components.

beryllium copper tube high performance becu alloy tubes

Dimension

round

OD:2mm-910mm, etc

WT:0.2mm-120mm, etc

Length: 1~12m, or in coil type, etc

square

Size:2mm*2mm-1016mm*1016mm, etc

WT:0.2mm-120mm, etc

Length: 1~12m, etc

rectangular

Size:2mm*2mm-1016mm*1219mm, etc

WT:0.2mm-120mm, etc

Length: 1~12m, etc

Hardness / Temper

1/16 hard,1/8 hard,3/8 hard,1/4 hard,1/2hard,full hard,soft,etc

Surface

mill,polished,bright,brushed,or as required

| Standard | GB/T1527-2006,JIS H3300-2006,ASTM B75M,ASTMB42,ASTMB111,ASTMB395, ASTM B359,ASTM B188,ASTM B698,ASTM B640,etc |
| --- | --- |

What is a beryllium copper tube?

A beryllium copper tube is a copper alloy tube with beryllium as the main alloying element, also known as beryllium bronze tube. Beryllium copper alloy is the best advanced elastic material among copper alloys, featuring extremely high strength, hardness, elasticity, electrical conductivity, thermal conductivity, wear resistance, corrosion resistance and fatigue resistance. Through solid solution and aging heat treatment, it can achieve strength close to that of steel while maintaining the electrical and thermal conductivity advantages of copper, and is widely used in high-precision and high-demand industrial fields.

Main performance and features

High strength and high hardness

Tensile strength ≥ 1000 MPa, hardness can reach 36-42 HRC (after heat treatment).

High conductivity and thermal conductivity

The conductivity is approximately 20-28% IACS, and the thermal conductivity is high. It is suitable for applications requiring high thermal and electrical conductivity.

Corrosion-resistant, fatigue-resistant, high-temperature resistant

It exhibits excellent corrosion resistance in the atmosphere, fresh water, seawater and various chemical media, has high fatigue strength, and excellent high-temperature stability.

Non-magnetic, shock-resistant, no spark generation

Suitable for explosion-proof and non-magnetic environments, such as mines, petroleum, precision instruments, etc.

The processing performance is excellent.

It can be used for turning, milling, drilling, welding, electroplating, etc., and supports customized processing of complex shapes.

Main applications

Beryllium copper tubes are widely used in the following fields:

Aerospace: for high-strength, high-conductivity, corrosion-resistant components such as heat exchangers, submarine cable relay housings, etc.

Electronics and electrical appliances: such as micro-motor brushes, connectors, springs, relays, electrodes, high-precision connectors, etc.

Mold manufacturing: for injection molds, die-casting core rods, high-precision mold inserts, etc., to improve heat dissipation and lifespan.

Welding industry: resistance welding electrodes, welding tools, etc.

Petroleum, chemical, medical: corrosion-resistant pipe fittings, instrument parts, explosion-proof tools, etc.

Automobile, machinery: bearings, bearing shells, gears, wear-resistant bushings, etc.

Common grades:

C17200: High-strength type, with the best comprehensive performance and the widest range of applications, suitable for high-load, high elasticity, and high conductivity scenarios.

C17300: Easy-to-machine type, containing a small amount of lead, suitable for automatic lathe processing, used for precision parts.

C17500/C17510: High conductivity type, mainly used for electrodes, high conductivity connectors, heat sinks, etc.

Common size range

Beryllium copper tubes (taking mainstream brands such as C17200, C17300, C17500 as examples) are widely used in precision electronics, molds, aerospace, and other fields. Their size range is extremely wide and can be customized according to actual needs. The following are the common size ranges of authoritative manufacturers and industry standards:

1. Regular beryllium copper tubes (general type)

Outer diameter (OD): 6 mm ~ 530 mm

Wall thickness (WT): 0.5 mm ~ 50 mm

Length: 1 m ~ 12 m (customizable to the required length)

Reference source: Yehan Industry (Shanghai) Co., Ltd., Shanghai Nonferrous Metals Network 3

2. Capillary beryllium copper tubes (precision type)

Outer diameter (OD): 0.3 mm ~ 3 mm

Wall thickness (WT): 0.03 mm ~ 0.3 mm

Tolerance: Tolerance of inner diameter or wall thickness can be achieved within 0.005 mm

Length: Customizable as per requirements

Reference source: Professional copper tube manufacturer on Douyin and capillary tube specification page 16

3. Thick-walled/ large-diameter beryllium copper tubes (industrial type)

Outer diameter (OD): up to 800 mm

Inner diameter (ID): up to 400 mm

Wall thickness: Customizable as per requirements, maximum up to 50 mm

Length: 1 m ~ 12 m